TECHNICAL DATA SHEET

Pigment Yellow 93

- Product Name

Trade Name: Disazo Yellow 93

C.I.: Pigment Yellow 93

C.I. No.: 20710

CAS No.: 5580-57-4

Molecular Formula: C43H35CL5N8O6

Formula Weight: 937.05

2. Physical, Chemical and Resistance Properties

Appearance: Yellow Powder

Shade: Similar to Standard

Density (g/cm3):1.5

Moisture: ≤1.5

Fineness(80 Mesh): ≤5.0

PH Value: 7

Water Soluble Matter (%): ≤2.0

Oil Absorption (ml/100g): ≤70

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 5

Water Resistance: 5

Oil Resistance: 5

Heat Resistance (℃): 200

Light Fastness (8=excellent): 7

3. Application

Application:plastic,water-base coating, solvent-base coating,

water-base ink,solvent-base ink,offset ink

4．Packing

Packed in 25kgs Bag with Pallet.