TECHNICAL DATA SHEET

Pigment Yellow 95

- Product Name

Trade Name: Disazo Yellow GR

C.I.: Pigment Yellow 95

C.I. No.: 20034

CAS No.: 5580-80-8

Molecular Formula: C44H38CL4N8O6

Formula Weight: 916.63

Chemical Class:Azo condensation

2. Physical, Chemical and Resistance Properties

Appearance: Yellow Powder

Shade: Similar to Standard

Density (g/cm3):1.4

Moisture: ≤1.5

Fineness(80 Mesh): ≤5.0

PH Value: 7

Water Soluble Matter (%): ≤2.0

Oil Absorption (ml/100g): ≤70

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 5

Water Resistance: 5

Oil Resistance: 5

Heat Resistance (℃): 200

Light Fastness (8=excellent): 7

3. Application

Application:plastic,water-base coating, solvent-base coating,

water-base ink,solvent-base ink,offset ink

4．Packing

Packed in 25kgs Bag with Pallet.