TECHNICAL DATA SHEET

Pigment Yellow 168

- Product Name

Trade Name: Permanent Yellow YT

C.I.: Pigment Yellow 168

C.I. No.: 13960

CAS No.: 71832-85-4

Molecular Formula: C16H13ClN4O7S

Formula Weight: 440.82

Chemical Class: Azo condensation

2. Physical, Chemical and Resistance Properties

Appearance: Yellow Powder

Shade: Similar to Standard

Density (g/cm3):1.5

Moisture: ≤1.5

Fineness(80 Mesh): ≤5.0

PH Value: 7

Water Soluble Matter (%): ≤2.0

Oil Absorption (ml/100g): ≤45

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 5

Water Resistance: 5

Oil Resistance: 4

Heat Resistance (℃): 210

Light Fastness (8=excellent): 7

3. Application

Application:plastic

4．Packing

Packed in 25kgs Bag with Pallet.