TECHNICAL DATA SHEET

Pigment Orange 43

- Product Name

Trade Name: Perinone Orange

C.I.: Pigment Orange 43

C.I. No.: 71105

CAS No.: 4424-06-0

Chemical Formula: C26H12N4O2

Molecular Weight: 412.4

2. Physical, Chemical and Resistance Properties

Appearance: Orange Powder

Shade: Similar to Standard

Density (g/cm3): 1.45

Moisture: ≤3%

Fineness(80 Mesh): ≤5%

PH Value: 6.5-7.5

Oil Absorption (ml/100g): 65-85

Water Soluble Matter (%): ≤1.5

Electric Conductivity (us/cm): ≤500

Acid Resistance: 3

Alkali Resistance: 3

Water Resistance: 4

Oil Resistance: 4

Heat Resistance (℃): 300

Light Fastness (8=excellent): 7

3. Application

Application: plastic, solvent-base paint,water-base paint,water-base ink, solvent-base ink,offset ink

4．Packing

Packed in 25kgs Bag with Pallet.