TECHNICAL DATA SHEET

Pigment Orange 62

- Product Name

Trade Name: Benzimidazolone Orange H5G

C.I.: Pigment Orange 62

C.I. No.: 11775

CAS No.: 52846-56-7

Chemical Formula: C17H14N6O5

Molecular Weight: 382.33

2. Physical, Chemical and Resistance Properties

Appearance: Orange Powder

Shade: Similar to Standard

Density (g/cm3): 1.52

Moisture: ≤3%

Fineness(80 Mesh): ≤5%

PH Value: 7

Oil Absorption (ml/100g): ≤70

Water Soluble Matter (%): ≤1.5

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 5

Water Resistance: 5

Oil Resistance: 5

Heat Resistance (℃): 180

Light Fastness (8=excellent): 7

3. Application

Application:solvent-base paint,water-base paint,water-base ink, solvent-base ink,offset ink

4．Packing

Packed in 25kgs Bag with Pallet.