TECHNICAL DATA SHEET

Pigment Orange 73

- Product Name

Trade Name: Irgazin ZPP Orange 16A

C.I.: Pigment Orange 73

C.I. No.: 561170

CAS No.: 084632-59-7

Chemical Formula: C26H28N2O2

Molecular Weight: 400.51

2. Physical, Chemical and Resistance Properties

Appearance: Orange Powder

Shade: Similar to Standard

Density (g/cm3): 1.2

Moisture: ≤3%

Fineness(80 Mesh): ≤5%

PH Value: 7

Oil Absorption (ml/100g): ≤50

Water Soluble Matter (%): ≤1.5

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 4

Water Resistance: 5

Oil Resistance: 5

Heat Resistance (℃): 200

Light Fastness (8=excellent): 7

3. Application

Application:Solvent-base paint,water-base paint

Recommended Application:Water-base ink, solvent-base ink,offset ink

4．Packing

Packed in 25kgs Bag with Pallet.