TECHNICAL DATA SHEET

Pigment Red 23

- Product Name

Trade Name: Naphthol Red

C.I.: Pigment Red 23

C.I. No.: 12355

CAS No.: 6471-49-4

Chemical Formula: C24H17N5O7

Molecular Weight: 487.42

2. Physical, Chemical and Resistance Properties

Appearance: Red Powder

Shade: Similar to Standard

Moisture: ≤1%

Fineness(80 Mesh): ≤5%

PH Value: 7

Water Soluble Matter (%): ≤1.5

Oil Absorption (ml/100g): ≤50

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 4

Water Resistance: 5

Oil Resistance: 3

Heat Resistance (℃): 130

Light Fastness (8=excellent): 6

3. Application

Application: solvent-base ink

4．Packing

Packed in 25kgs Bag with Pallet.