TECHNICAL DATA SHEET

Pigment Red 48:3

- Product Name

Trade Name: Fast Red 2BS-P

C.I.: Pigment Red 48:3

C.I.No.:15865:3

CAS Number: 15782-05-5

Chemical Formula: C18H11ClN2O6SSr

Molecular Weight: 506.44

EU Number: 239-879-2

2. Physical, Chemical and Resistance Properties

Appearance: Red Powder

Shade: Similar to Standard

Tinting Strength:100%

Bulk Density(lb/gal): 13.4-15.8

Density (g/cm3): 1.78

Moisture: ≤1%

Fineness(80 Mesh): ≤5%

PH Value: 7.0-8.5

Oil Absorption (ml/100g): 45±5

Water-soluble Matter (%): ≤2.5

Heat Resistance: 190℃

Light Fastness: 8

Oil Resistance: 4

Acid Resistance: 5

Alkali Resistance: 3

Water Resistance: 4

Oil Resistance: 5

Alcohol Resistance: 4

Water Resistance: 4

3. Application

Application: plastic

4．Packing

Packed in 25kgs Bag with Pallet.