TECHNICAL DATA SHEET

Pigment Red 52:2

- Product Name

Color Index: Pigment Red 52:2

C.I. No.: 15860:2

CAS No.: 12238-31-2

Chemical Group: BONS Mn

2. Physical, Chemical and Resistance Properties

Moisture (%): ≤3.0

Water Soluble Matter (%): ≤2.5

Oil Absorption (ml/100g): 45-55

Electric Conductivity (us/cm): ≤500

Fineness (80mesh) %: ≤5.0

PH Value: 6.5-7.5

Acid Resistance: 5

Alkali Resistance: 5

Alcohol Resistance: 5

Ester Resistance: 5

Benzene Resistance: 5

Bleeding Resistance: 5

Heat Resistance (℃): 180

Light Fastness (8=excellent): 6

3. Application

Recommended for Industrial Paint. Suggested for Solvent Based Decorative Paint.

4. Technical properties

With good performance.