TECHNICAL DATA SHEET

Pigment Red 31

- Product Name

Trade Name: Naphthol Red 31

C.I.: Pigment Red 31

C.I. No.: 12360

CAS No.: 6448-96-0

Chemical Formula: C31H23N5O6

Molecular Weight: 561.54

2. Physical, Chemical and Resistance Properties

Appearance: Red Powder

Shade: Similar to Standard

Moisture: ≤1%

Fineness(80 Mesh): ≤5%

PH Value: 7

Water Soluble Matter (%): ≤1.5

Oil Absorption (ml/100g): ≤50

Electric Conductivity (us/cm): ≤500

Acid Resistance: 5

Alkali Resistance: 5

Water Resistance: 5

Oil Resistance: 4

Heat Resistance (℃): 150

Light Fastness (8=excellent): 7

3. Application

Application: Printing

Recommended Aplication:Water-base ink

4．Packing

Packed in 25kgs Bag with Pallet.