TECHNICAL DATA SHEET

Pigment Red 202

- Product Name

Trade Name: Quinaridone Magenta 202

C.I.: Pigment Red 202

C.I. No.: 73907

CAS Number: 3089-17-6

Molecular Formula: C20H10CL2N2O2

Molecular Weight: 381.21

2. Physical, Chemical and Resistance Properties

Appearance: Red Powder

Shade: Similar to Standard

Tinting Strength:100%

Fineness (80mesh) %: ≤5

Moisture (%):≤1.5

PH Value:  7

Oil Absorption (ml/100g): ≤70

Light Fastness: 7-8

Heat Resistance: 200

Water Resistance: 5

Oil Resistance: 5

Acid Resistance: 5

Alkali Resistance: 5

- Application

Application:Plastic,water-base paint,Solvent-base paint, water-base ink, Solvent-base ink, offset ink

4．Packing

Packed in 25kgs Bag with Pallet.