TECHNICAL DATA SHEET

Pigment Red 214

- Product Name

Trade Name: Cromophtal Red BN

C.I.: Pigment Red 214

C.I. No.: 200660

CAS Number: 40618-31-3

Molecular Formula: C40H22CL6N6O4

Molecular Weight: 863.36

2. Physical, Chemical and Resistance Properties

Appearance: Red Powder

Shade: Similar to Standard

Tinting Strength:100%

Fineness (80mesh) %: ≤5

Moisture (%):≤1.5

PH Value:  7

Oil Absorption (ml/100g): ≤70

Light Fastness: 7

Heat Resistance: 250

Water Resistance: 5

Oil Resistance: 5

Acid Resistance: 5

Alkali Resistance: 5

- Application

Application: Water-based paint,Solvent-base paint

Recommended Application:Water-based Ink, Solvent-base ink,offset

4．Packing

Packed in 25kgs Bag with Pallet.