TECHNICAL DATA SHEET

Pigment Red 242

- Product Name

Trade Name: Sandorin Scarlet 4RF

C.I.: Pigment Red 242

C.I. No.: 20067

CAS Number: 52238-92-3

Molecular Formula: C42H22Cl4F6N6O4

Molecular Weight: 930.46

2. Physical, Chemical and Resistance Properties

Appearance: Red Powder

Shade: Similar to Standard

Tinting Strength:100%

Bulk Density(lb/gal): 12.5

Density (g/cm3): 1.57

Fineness (80mesh) %: ≤5

Moisture (%):≤1.5

PH Value:  7

Oil Absorption (ml/100g): ≤60

Light Fastness: 7

Heat Resistance: 200

Water Resistance: 5

Oil Resistance: 5

Acid Resistance: 5

Alkali Resistance: 5

- Application

Application:Plastic,water-base paint,Solvent-base paint, water-base ink, Solvent-base ink, offset ink

4．Packing

Packed in 25kgs Bag with Pallet.